## Slide 1: Carbon Footprint Reduction in Construction using Geopolymer Cement
JEBIN RAJ. J
SANJANA. A
ANTO AAKASH. M

## Slide 2
Elevator pitch
We make eco-friendly geopolymer bricks by reusing industrial waste materials such as fly ash and GGBS. Instead of burning clay or using high-carbon cement, we mix these materials with alkaline solutions to form a strong and durable binder. This process avoids the large energy use and carbon emissions linked to traditional brick making and also prevents soil damage. At the same time, it helps industries manage their by-products more responsibly. The result is a low-cost brick with excellent resistance to water, fire, and chemicals. Our approach can support construction firms, sustainable housing projects, and green building developers who need reliable materials that align with global environmental goals.

## Slide 3
Methodology
Collect Raw Materials:
Fly ash (Class F), GGBS, sodium hydroxide (NaOH), sodium silicate (Na₂SiO₃), sand, and water.
Prepare Alkaline Activator:
Mix NaOH solution (e.g., 10M) with Na₂SiO₃ in a 2.5:1 ratio and allow the solution to rest for 24 hours.
Mixing:
The fly ash and GGBS are combined in a desired ratio and also gradually add the alkaline solution and mix thoroughly. add sand if needed.
Brick Casting:
The fresh mix is poured into standard brick moulds (230×110×75 mm) after that compact properly to remove air voids.

## Slide 4
Curing:
Curing At room temperature for 7 or 28 days (ambient curing). And the alternative method is bricks are placed in the oven at the temperature of (60°C to 80°C) for 24 or 48 hours
Testing:
Test the bricks for compressive strength, water absorption, size and surface quality
Compare Results:
Compare the performance of geopolymer bricks with conventional OPC bricks and Estimate potential CO₂ emission reduction

## Slide 5
Problems
1) Conventional clay & OPC bricks → high CO₂ emissions (~8% globally)
2) Clay extraction damages topsoil
3) OPC manufacturing burns limestone at high heat → massive energy use
4) Industrial waste (fly ash, GGBS) piles up → land & water pollution
Solution
1) Convert fly ash & GGBS into geopolymer bricks
2) No high-heat kilns → lower energy + fewer emissions
3) Stronger, denser, water/fire/chemical resistant bricks

## Slide 6
Market Opportunity
India’s construction sector is booming, already valued at more than ₹11 trillion, and it shows no signs of slowing down thanks to rapid urban growth and ongoing housing initiatives. Bricks, a staple in every building project, represent a large share of this market, with billions produced annually. At present, the majority come from clay or OPC-based cement, but both face increasing challenges rising raw material costs, environmental concerns, and tighter regulations. These factors are paving the way for cleaner alternatives. Geopolymer bricks step in as a practical solution, matching the strength and performance of traditional bricks while slashing carbon emissions and making productive use of industrial waste. With government policies pushing for greener infrastructure and builders actively seeking cost-effective, durable products, the potential demand for geopolymer bricks is not just significant it’s growing steadily year after year.

## Slide 7
Product cost
The cost of the one geopolymer brick is approximately 8 to 10 Rs
Component | Quantity | Estimated Cost (INR)
Fly ash | 3,000 kg | 3,000
GGBS | 2,000Kg | 4,000
Alkaline Activators | - | 12,000
Water | 2,000 liters | 500
Labour | - | 15,000
Electricity for Curing | - | 5,000
Moulds and Tools | - | 3,000
Total cost | - | 50,000

## Slide 8
Chart: Testing
| Compressive strength | Water Absorption | Tensile strength | Acid Resistance(HCl)
Geopolymer bricks | 16.11 | 1.44 | 2.59 | 0.32
Traditional bricks | 12.46 | 10.74 | 1.15 | 2.65

## Slide 9
Chart: Carbon emission comparsion
| Raw materials | Binder production | Manufacturing energy use | Other associated pollutants
Geopolymer bricks | 0.05 | 0.2 | 0.1 | 0.02
Traditional bricks | 0.15 | 0.3 | 0.04 | 0.1

## Slide 10
References
C. Antony Jeyasehar1, G. Saravanan2 A.K. Ramakrishnan1 and S. Kandasamy3 strength and durability studies on fly ash based geopolymer bricks
H. M. Khater, M.Ezzat and A. M. El Nagar engineering of low cost geopolymer building bricks applied for various construction purposes
Raghulkumar. R1, Thirugnanasambandam. S2 study on conventional and geopolymer bricks
Nicolas Youssef 1 ,2,*, Andry Zaid Rabenantoandro1, Zakaria Dakhli1, Fadi Hage Chehade2, and Zoubeir Lafhaj1 Environmental evaluation of geopolymer bricks
Yuxin (Justin) Wang * and Hossam Abuel-Naga Unfired Bricks from Wastes: A Review of Stabiliser Technologies, Performance Metrics, and Circular Economy Pathways
Marwa Dabaieh a,b,*, Jukka Heinonen c, Deena El-Mahdy d, Dalya M. Hassan dA comparative study of life cycle carbon emissions and embodied energy between sun-dried bricks and fired clay bricks

## Slide 11
THANK YOU